WEATHERCOAT STONESHIELD GLAZE COAT (WB)

Product Description

A high performance coating based on pure acrylic resin, water repellent and UV resistant compounds to provide a tough durable composite coating for our Stoneshield system.

Recommended Areas of Application

Area of Use: Interior and exterior

Substrate: Concrete, Plaster and Masonry.

Technical Data

Sheen Variants: Smooth

Colours: White

Volume Solids: 26 ± 2%

Theoretical Covering Capacity: 6 Sqm/Ltr.

Practical Covering Capacity

For estimation of practical covering capacity, following factors to be taken into account: surface profile, uneven application, over spray, losses in container and equipment etc.

| Drying time | Substrate Temp. | Touch Dry | Overcoating Interval |  |
| --- | --- | --- | --- | --- |
|  |  |  | Minimum | Maximum |
|  | 25°C | 30 minutes | 8 hours | Indefinite |
|  | 35°C | 20 minutes | 6 hours | Indefinite |
|  | 45°C | 15 minutes | 4 hours | Indefinite |

Application Data

Method of Application		:	Roller or brush

Thinner				:	Sweet water

Thinning Ratio (by vol.)		:	Use 5% to 10% sweet water for ease of application depending on application.

Application Details

• Ensure adequate ventilation during application and drying

• Do not apply when humidity exceeds 85% and condensation is likely

• Surface temperature should be 3°C or more above dew point

TYPICAL PAINT SYSTEM

Interior

1 coat x Weathercoat Stoneshield Primary Coat

2 coats x Weathercoat Stoneshield Secondary Coat

1or 2 coats x Weathercoat Stoneshield Glaze Coat

For alternate system suggestion please contact Berger Paints Sales Representative

Storage, Safety Information and Precautions

• Keep out of reach of children.

• Store in cool, dry conditions; ensure adequate ventilation during application.

• Avoid contact with skin and eyes; wear suitable protective clothing such as overalls, goggles, dust masks and gloves.

• Shelf life up to 12 month is from the date of manufacture.

• Flash Point: NA

First-Aid

• Eyes: In the event of accidental splashes, flush eyes immediately with warm water and obtain medical advice.

• Skin: Wash skin thoroughly with soap and water, or with an approved industrial cleaner. Do not use solvents.

• Inhalation: Move patient to fresh air, loosen collar and keep patient rested.

• Ingestion: Do not induce vomiting. Obtain immediate medical attention.

• Dispose in landfill only.

Disclaimer

The information provided in this data sheet is not intended to be complete. It is the responsibility of the user to ensure that the product used is suitable for the purpose it is meant to serve. In view of various factors affecting the performance of the coating, we cannot assume responsibility for the product performance, nor do we accept any liability arising from use of this product, unless specifically agreed to in writing by us. The information provided in the datasheet may be modified by us without notice.