SYSTEM: PREMIUM STONE FINISH - EXTERIOR

Concrete and Masonry Surface – Exteriors

System Description

Primary Coat: 1 coat of Weathercoat Stone Shield Primer Water thinnable coating with good alkali resisting properties designed to provide a sound base to stone shield secondary coat.

Volume Solids: 26% ± 2%

VOC: <28.6 gms/ltr complies to LEED Standard

Secondary Coat: 2 coats of Weathercoat Stone Shield

Weathercoat Stoneshield Secondary Coat is a water thinnable textured coating containing high quality quartz aggregates and coloured quartz chips which gives an excellent natural engraved look with high level of aesthetic appeal. In addition this product is based on a pure and 100% acrylic binder along with reinforced quartz chips as mentioned above. In combination with Weathercoat Stone Shield Primary and Weathercoat Stone Shield Glaze Coat, it provides the following benefits.

• Excellent adhesion to the masonry substrate

• Low maintenance costs

• Resistant to environmental pollutant and chemicals

• Environment friendly

• Excellent reduction in water absorption

Volume Solids: 63% ± 2%

VOC: <21.2 gms/ltr complies to LEED Standard

Top Coat: 2 coats of Weathercoat Stone Shield Glaze Coat

A high performance coating based on pure acrylic resin, water repellent and UV resistant compound to provide a tough durable composite coating for stone shield system

Volume Solids: 26% ± 2%

VOC: <0.08 gms/ltr complies to LEED Standard

Certificate

Adhesion test: Value 0.5 N/mm2, Test Method-ASTM D 4541: 2002

Abrasion Resistance: 151 gms weight loss after 1000 cycles (1kg Load / Cs - 17 wheel)

Freeze Thaw Resistance: No changes Observed, Test Method - ASTM D 2243 - 90

Falling Weight Test: No sign of Cracks or Disbonding Observed, Test Method - ISO 6272 - 93

Alkali Resistance: No changes Observed, Test Method - ASTM D 543

UV Resistance: Passes 500 Hrs, Test Method - ASTM G 53: 88

Water Permeability: 100% Reduction, Test Method - BS EN 12390 - 8: 2009

Recommended Areas of Application

Area of Use: Exterior only

Substrate: Concrete and brick walls, plastered surfaces and masonry surfaces.