WEATHERCOAT VINTAGE GLAZE COAT (WB)

Product Description

A high performance coating containing water repellent and UV resistant compounds to provide a tough, durable composite coating for our Vintage system.

Recommended Areas of Application

Area of Use: Interior and exterior

Substrate: Concrete, Plaster and Masonry

Technical Data

Finish: Matt, Smooth

Colours: Clear

Solids (% by volume): 25± 2

Thinner/Cleaner: Sweet water

Theoretical Spread Rate: 6-10sqm. per litre depending on profile of stone finish

Practical Spread Rate

While estimating the practical spread rates, due allowance should be made for surface profile of the secondary coat and the absorption of the glaze coat into secondary coat.

| Drying time | Substrate Temp. | Touch Dry | Overcoating Interval |  |
| --- | --- | --- | --- | --- |
|  |  |  | Minimum | Maximum |
|  | 35°C | 20 minutes | 2 hours | Indefinite |

Storage and Handling

Storage: Store in cool, dry conditions.

Disposal: Dispose as normal paints e.g. by controlled landfill. In case of doubt, consult local authority. Do not empty into drains, sewers or other water courses.

Flash Point: N/A

Shell Life: Upto 12 months

Application Method

Ensure adequate ventilation during application and drying. Do not apply when humidity exceeds 85% and condensation is likely. Only apply coating when surface temperature should be 3°C or more above dew point. Use 5% to 10%thinner for ease of application depending on the method of application.

Brush or Roller: Apply an even coat taking care to avoid runs and sags.

Safety Precautions

• Avoid contact with the skin and eyes. Wear suitable protective clothing such as overalls, goggles, dust masks and gloves. Use a barrier cream.

• Ensure that there is adequate ventilation in the area where the product is being applied. Do not breathe vapour or spray.

• Refer to MSDS for safe handling and application of this product.

First-Aid

• Eyes: In the event of accidental splashes, flush eyes immediately with warm water and obtain medical advice.

• Skin: Wash skin thoroughly with soap and water, or with an approved industrial cleaner. Do not use solvents.

• Inhalation: Remove to fresh air, loosen collar and keep patient rested.

• Ingestion: In case of accidental ingestion do not induce vomiting. Obtain immediate medical attention.

Disclaimer

The information provided in this data sheet is not intended to be complete. It is the responsibility of the user to ensure that the product used is suitable for the purpose it is meant to serve. In view of various factors affecting the performance of the coating, we cannot assume responsibility for the product performance, nor do we accept any liability arising from use of this product, unless specifically agreed to in writing by us. The information provided in the datasheet may be modified by us without notice.