SYSTEM: DURABLE MEDIUM TEXTURE FOR EXTERIORS

Concrete and Masonry Surface – Exterior

System Description

Primary Coat: 1 coat Weathercoat AR Primer

A premium quality acrylic co-polymer based primer with good alkali resisting properties designed to provide a sound base for texture coating from the Berger range.

Volume Solids: 40% ± 2%

Top Coat: 2 coats of Select Medium Texture

A medium texture coating based on a tough, durable acrylic co-polymer resin, pigmented with titanium dioxide and other light fast alkali resisting pigments, and reinforced with selected mineral quartz and mica. Its formulation incorporating fungicides and algaecides, and its build ensure good weather resistance and also helps cover hairline surface cracks and irregularities.

Volume Solids: 56% ± 2%

Recommended Areas of Application

Area of Use: Exterior & Interior

Substrate: Concrete, Plaster, Masonry, Brickwork, Block work, Gypsum, Timber.