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SELECT TARTARUGA ROUGHCAST
Product Description
Tartaruga Roughcast is a synthetic render-cum-finish which can be applied straight to most fairface surface such as concrete, plaster, brick work both exterior and interior. Tartaruga Roughcast is ready mixed coating composed of high quality exterior durable polymer reason, and weather resistant pigments, incorporating special graded marble granules. With its unique engraved finish, Tartaruga Roughcast is truly a decorative plaster and superb finish both in one. Tartaruga Roughcast most effectively combines the decorative appeal of a unique finish with the anti carbonation performance of the coating. Tartaruga Roughcast incorporates specially selected fungicides and algaecides which reduce efflorescence, resist alkaline hydrolysis, tropical fugas, algae and mould growth, both on the surface and beneath. Tartaruga Roughcast has excellent ultra violet resistance, adhesion on various surface and color retention. Tartaruga Roughcast has a breathable film that breathes out trapped moisture both from the paint surface as well as the substrate

Recommended Areas of Application
Area of Use: Interior and exterior

Technical Data
Sheen Variants: Unique engraved finish, Matt
Colours: White, other colors on request
Volume Solids: 75 ± 2%
	Theoretical Covering Capacity

	Depends on the surface profile and coat thickness. For a reasonable fairface surface, 0.5-0.75 m2 per litre may be achieved for a coat thickness of up to 2 mm



	Practical Covering Capacity

	For estimation of practical covering capacity, following factors to be taken into account: Surface profile, uneven application, over spray, losses in container and equipment etc.



	


Drying time
	Substrate Temp.
	Touch Dry
	Over coating Interval

	
	
	
	Minimum
	Maximum

	
	25°C
	4 hours
	24 hours
	Indefinite

	
	35°C
	3 hour
	20 hours
	Indefinite

	
	45°C
	2 Hour
	16 hours
	Indefinite


Application Data
Method of Application		:	Trowel, Spatula
Thinner				:	Sweet water
Thinning Ratio (by vol.)		:	N/A
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Surface Preparation
The performance of this coating is directly related to the degree of surface preparation.
• Ensure surface is clean, dry and free from all contaminants.
• Surface must be sound and free from laitance.
• Remove laitance by wire brush or sweep blast.
Note: Dusting or chalking surface should be consolidated using Plastaseal Penetrating Sealer

Application Details
• Ensure adequate ventilation during application and drying.
• Do not apply when humidity exceeds 85% and condensation is likely.
• Surface temperature should be 3°C or more above dew point.
• Stir the contents thoroughly before and during use, with a broad flat stirrer, using and upward lifting action.
• Apply Rustic Decor by a trowel or a spatula or even a roller to obtain an even coating of around 1 mm thickness.
• Allow to set for 5-15 minutes.
• Rub the face of the applied area with a stainless steel of plastic trowel, which will roll on the coarsest grains in the coating and produce the desired engraved finish.
Note: Depending on the area of use, other systems can be recommended.

	TYPICAL PAINT SYSTEM

	Interior

	1 coat x Berger Alkali Resistant Primer

	1coat x Select Tartaruga roughcast

	For alternate system suggestion please contact Berger Paints Sales Representative



Storage, Safety Information and Precautions
• Keep out of reach of children.
• Store in cool, dry conditions; ensure adequate ventilation during application.
• Shelf life up to 12 months from the date of manufacture.
• Avoid contact with skin and eyes; wear suitable protective clothing such as overalls, goggles, dust masks and gloves.

First-Aid
• Eyes: In the event of accidental splashes, flush eyes immediately with warm water and obtain medical advice.
• Skin: Wash skin thoroughly with soap and water, or with an approved industrial cleaner. Do not use solvents.
• Inhalation: Move patient to fresh air, loosen collar and keep patient rested.
• Ingestion: Do not induce vomiting. Obtain immediate medical attention.
• Dispose in landfill only.

Disclaimer
The information provided in this data sheet is not intended to be complete. It is the responsibility of the user to ensure that the product used is suitable for the purpose it is meant to serve. In view of various factors affecting the performance of the coating, we cannot assume responsibility for the product performance, nor do we accept any liability arising from use of this product, unless specifically agreed to in writing by us. The information provided in the datasheet may be modified by us without notice.
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