SYSTEM: WATER BASE ANTI - CARBONATION FINISH - SMOOTH

Concrete and Masonry Surface – Exteriors

System Description

Primary Coat: 1 coat of TUFF AR Primer

A water based primer based on NANO acrylic emulsion pigmented with titanium dioxide and other light fast and alkali resisting pigments. Due to its superior design and consistency when properly applied this is capable of a giving maximum spreading rate of 100 sqm per 20 kg per two coats.

Volume Solids: 30% ± 2%

Top Coat: 2 coats of TUFF Exterior Emulsion

An emulsion based on NANO acrylic emulsion pigmented with titanium dioxide and other light fast and alkali resisting pigments. Due to its superior design and consistency when properly applied this is capable of a giving maximum spreading rate of 120 sqm per 20 kg per two coats. Further Tuff Exterior emulsion provides excellent long lasting adhesion on variety of textured surface coupled with good anti-microbial resistance. In addition its high scrub resistance due to excellent binding capability of NANO emulsion makes it ideal for tough Middle East Climate. Further it has excellent UV resistance to provide a long lasting aesthetics to exterior facades.

Volume Solids: 44% ± 2% (Matt), 35% ± 2% (Shyne)

Sheen Variant: MATT and SHYNE

Certificates

• Wet Scrub resistance Test: ASTM ( D 2486) Passes 6150 Scrubs

• UV Resistance Test : ASTM G 154:06 – Passes 2000 Hours of UV exposure @ 60 Degree

• Fire Resistance : BS 476 -Certifies by Exova Warrington as Class 0 Product

• Anti Carbonation : TP 950/05/13569 in Accordance with EN 1062-6 : 2002.

• SD Value, (R- Value) – 119 @ 104 DFT.

• Solar Reflectance (%) as per ASTM C 1549 - 09, Value: 84.7%

Recommended Areas of Application

Area of Use: Exterior only

Substrate: Concrete, Plaster, Masonry, Gypsum, Timber.