SYSTEM : PREMIUM ANTI -CARBONATION ELASTOMERIC FINISH - SMOOTH

Concrete and Masonry Surface –Exterior

System Description

Primary Coat: 1 coat of Weather Coat Flex Primer

Environment friendly, water-based 100% acrylic sealer with excellent adhesion and penetration to concrete, brick wall and plastered surfaces.

Volume Solids: 35% ± 2%

Top Coat: 2 coats of Weathercoat Flex Smooth Emulsion

Ultra high performance formulation based on pure and 100% acrylic emulsion high quality colour stable and durable pigments. Its special formulation incorporating fungicides and algaecides ensures outstanding exterior durability combined with excellent light fastness assures a durable long lasting aesthetic finish with silky sheen.

Highlights:

• Outstanding exterior durability

• Environment friendly

• Excellent resistance against dirt pick-up

• Low toxicity and odour

• Good protection against carbonation

• Resistance to fungi and algae

Volume Solids: 55% ± 2%

Certificates

Elongation at break as per test method ASTM D638:02A	:	269%

Carbon dioxide diffusion					:	Equivalent air layer thickness (R) = 166 mt

Breathability [water vapour transmission]			:	Equivalent air layer thickness (Sd) = 0.8 mt.

Chloride permeability as per ASTM C1202:97		:	>95% reduction

Salt spray test						:	Passes 1000 Hrs, Test method ASTM B117 - 07A

Crack Bridging capacity					:	2.6mm, Test Method ASTM C 836: 95

Recommended Areas of Application

Area of Use: Exterior only

Substrate: Concrete and brick walls, plastered surfaces and masonry surfaces.