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	SYSTEM : PREMIUM ANTI -CARBONATION ELASTOMERIC FINISH - SMOOTH

	Concrete and Masonry Surface –Exterior



System Description
Primary Coat: 1 coat of Weather Coat Flex Primer 
Environment friendly, water-based 100% acrylic sealer with excellent adhesion and penetration to concrete, brick wall and plastered surfaces. 

Volume Solids: 35% ± 2%

Top Coat: 2 coats of Weathercoat Flex Smooth Emulsion 
Ultra high performance formulation based on pure and 100% acrylic emulsion high quality colour stable and durable pigments. Its special formulation incorporating fungicides and algaecides ensures outstanding exterior durability combined with excellent light fastness assures a durable long lasting aesthetic finish with silky sheen.

Highlights:
• Outstanding exterior durability
• Environment friendly
• Excellent resistance against dirt pick-up
• Low toxicity and odour
• Good protection against carbonation
• Resistance to fungi and algae
Volume Solids: 55% ± 2%
Certificates
Elongation at break as per test method ASTM D638:02A	:	269%
Carbon dioxide diffusion					:	Equivalent air layer thickness (R) = 166 mt
Breathability [water vapour transmission]			:	Equivalent air layer thickness (Sd) = 0.8 mt.
Chloride permeability as per ASTM C1202:97		:	>95% reduction
Salt spray test						:	Passes 1000 Hrs, Test method ASTM B117 - 07A
Crack Bridging capacity					:	2.6mm, Test Method ASTM C 836: 95

Recommended Areas of Application
Area of Use: Exterior only
Substrate: Concrete and brick walls, plastered surfaces and masonry surfaces.
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