SYSTEM: SOLVENT BASED ACRYLIC ANTI CARBONATION SYSTEM - EXTERIOR

Concrete and Masonry Surface – Exterior

System Description

Primary Coat: 1 coat Weathercoat AR Primer

A premium quality acrylic co-polymer based primer with good alkali resisting properties designed to provide a sound base for texture coating from the Berger range.

Volume Solids: 40% ± 2%

Secondary Coat: 1 coat of Weathercoat Acrylic Spray Compound

An acrylic co-polymer compound containing special grades of fine quartz aggregates primarily designed as an intermediate texture coating.

Volume Solids: 62% ± 2%

Top Coat: 2 coats of Weathercoat Luxacryl (High Gloss and Low Sheen)

A high performance thermoplastic, water repellent coating based on solvented acrylic polymer containing titanium dioxide and other high grade light fast pigments.

Volume Solids: 44% ± 2%

Certificates

Adhesion test: Value 1.0 N/mm2, Test Method - ASTM D 4541: 2002

Crack bridging capacity - VALUE - 1.84 MM, ASTM -C 836 : 2005, ASTM - C 1305 : 2008

TENSILE and ELONGATION: Tensile strenght = 1.5 N/mm2, Elongation % = 14, Test

Method - ASTM D 412

QUV Resistance: Passes 1000 Hrs, Test Method - G 154 - 06

Water Vapour Transmission: SD Value (M) = 0.117, Test Procedure TP/N950/09/16074

Water Permeability: 100% Reduction, Test Method - BS EN 12390 - 8: 2009

Shore A Hardness: Value = A/64/1, Test Method - ASTM D 2240 - 2005

Abrasion Resistance: 334 gms weight loss after 1000 cycles (1kg Load / Cs - 17 wheel)

Recommended Areas of Application

Area of Use: Exterior only

Substrate: Concrete and brick walls, plastered surfaces and masonry surfaces.