Concrete and Masonry Surface – Exteriors

SYSTEM : ANTI MICROBIALPREMIUM SMOOTH FINISH-EXTERIOR

System Description

Primary Coat: 1 coat of Weathercoat Primer

Water-based Alkali resistant primer with 100% acrylic sealer.

Volume Solids: 40% ± 2%

Secondary Coat: 2 coats of Weathercoat Smooth Emulsion (Matt)

A premium quality durable, smooth exterior coating based on a tough, pure and 100% acrylic resin, pigmented with titanium dioxide and other high grade light grade light fast alkali resisting pigment.

Volume Solids: 35% ± 2%

Certificate

MPI 10

Recommended Areas of Application

Area of Use: Exterior only

Substrate: Concrete and brick walls, plastered surfaces and masonry surfaces.