SYSTEM : EPOXY BASED FLOOR COATING FOR WAREHOUSES, FOOD PROCESSING, SOFT DRINKS, AUTOMOTIVE PLANTS AND CHEMICAL PLANTS

Floor- MD Indoor

System Description

Primary Coat: 1 coat of Apcoflor HFP 120 Clear @ 50 μ

Two component, high solid, epoxy resin based universal floor primer.

Volume Solids: 90% ± 2%

VOC: 7.1 gms/ltr, Test Method USEPA 24

Top Coat: 2 coats of Apcoflor TC-510 @ 250 μ

Two component, high build, solvent free, epoxy floor coating.

Volume Solids: 100% (Based on ASTM D2697)

VOC: 3.9 gms/ltr, Test Method USEPA 24

Certificate

• Shore ‘D’ Hardness: D/65/1, Test method - ASTM D 2240

• Compressive Strength - 70.1 N/mm2, Test method - ASTM C 579

• Flexural Strength: 40.1 N/mm2, Test method - ASTM C 580

• Tensile Strength: 20.1 N/mm2, Test method - ASTM C 307

• Impact Resistance: No sign of crack or disbonding observed, Test method - ASTM ISO 6272

• Crack Bridging Capacity: Value -1.10 mm, Test method - ASTM C 836:95

• Rapid Chloride Permeability: 96% reduction, Test method - ASTM C 1202.97

• Water Permeability: Nil, Test method - BS EN 12390 (PART 8 : 2000)

• Chemical Resistance: No change observed, Test method - ASTM D 543

• Hot Water Resistance: No change observed, Test method- ASTM D 570

• Abrasion Resistance: 134 gms weight Lost after 1000 Cycles (1 kg Load CS-17 Wheel)

Test Method - ASTM D 4060 : 01

• Anti-fungal test: No growth seen, Test method - D3273

• Anti-bacterial activity: Zero no. of colonies, Test method - ASTM D558

Designed Use

• Easy clean floor coating for food processing plants, soft drink plants

• Seamless automotive plants, warehouses and chemical plants.