[image: C:\Users\user\Desktop\Spec sheet Header.jpg]
	SYSTEM : FLOOR COATING FOR HEAVY DUTY RAMPS, FLOORING AND VEHICLE PARKING

	Floor - HD/VHD Indoor



System Description

Primary Coat: 1 coat of Apcoflor HFP 120 Clear @ 100 μ
Two component, high solid, epoxy resin based universal floor primer.

Volume Solids: 90% ± 2%
VOC: 7.1 gm / ltr, Test Method - USEPA 24

Top Coat: 1 coat of Apcoflor HSC-3 (Screed) @ 5000 μ
Three component, epoxy resin based floor screed.

Volume Solids: 100% (Based on ASTM - D2697)
VOC: <0.01(g/L) (Test Method -USEPA 24)

Certificates
Compressive Strength: 94.3 N/mm2, Test Method-ASTM C 579
Flexural Strength: 21.0 N/mm2, Test method - ASTM- C 580
Tensile Strength: 16.5 N/mm2, Test method - ASTM C 307
Rapid Chloride Permeability: 96 % Reduction, Test Method - ASTM 1202.97
Chemical Resistance: No Change Observed, Test Method - ASTM D 543
Hot water Resistance: No Change Observed, Test Method -ASTM D 570
Abrasion Resistance: 54.3 gms weight Lost after 1000 Cycles (1 kg Load CS-17 Wheel),
Test Method - ASTM 4060:01

Designed Use
• For heavy duty ramps, floorings and vehicle parking
• Loading unloading bays for heavy duty vehicles, high abrasion floors for engineering plants, workshops, dairies, breweries, food processing, automotive and chemical plants.
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