SYSTEM : EPOXY BASED FLOOR COATING FOR SHOWROOMS, BUSINESS CENTRES AND MALLS

Surface – GI

System Description

Primary Coat: 1 coat of Apcoflor HFP 120 Clear @ 50 μ

Two component, high solid, epoxy resin based universal floor primer.

Volume Solids: 90% ± 2%

VOC: 0.1gm/ltr, Test Method USEPA 24

Secondary Coat: 1 coat of Apcoflor SL-4 @ 3000 μ

Three component, epoxy resin based floor screed.

Volume Solids: 100% (Based on ASTM - D2697)

VOC: < 1gm/ltr, Test Method USEPA 24

Certificate

• Shore ‘D’ Hardness: Value D/55/1, Test Method - ASTM D 2240

• Compressive Strength: 20.8 N/mm2, Test Method - ASTM C 579

• Flexural Strength: Value 8.3 N/mm2, Test Method - ASTM C 580

• Tensile Strength: 5.5 N/mm2, Test method - ASTM C 307

• Impact Resistance: No sign of Crack or Disbonding observed, Test Method - ASTM ISO 6272

• Crack Bridging Capacity: Value -1.35 mm, Test Method - ASTM C 836:95

• Rapid Chloride Permeability: Value = 99% Reduction, Test Method - ASTM C 1202.97

• Water Permeability - BS EN 12390 (PART 8 : 2000)

• Chemical Resistance: No change observed, Test Method - ASTM D 543

• Hot Water Resistance: No change observed, Test Method - ASTM D 570

• Abrasion resistance: 107 gms weight Lost after 1000 Cycles ( 1 kg Load CS-17 Wheel) Test

Method - ASTM D 4060 : 01

Designed Use

• Seamless floorings for showrooms, business centres, malls

• Easy clean coating to kitchen and poultries.

• Pharmaceutical units, food processing plants and chemical plants.