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	SYSTEM : EPOXY BASED FLOOR COATING FOR SHOWROOMS, BUSINESS CENTRES AND MALLS

	Surface – GI



System Description

Primary Coat: 1 coat of Apcoflor HFP 120 Clear @ 50 μ 
Two component, high solid, epoxy resin based universal floor primer.

Volume Solids: 90% ± 2%
VOC: 0.1gm/ltr, Test Method USEPA 24

Secondary Coat: 1 coat of Apcoflor SL-4 @ 3000 μ 
Three component, epoxy resin based floor screed.

Volume Solids: 100% (Based on ASTM - D2697)
VOC: < 1gm/ltr, Test Method USEPA 24

Certificate
• Shore ‘D’ Hardness: Value D/55/1, Test Method - ASTM D 2240
• Compressive Strength: 20.8 N/mm2, Test Method - ASTM C 579
• Flexural Strength: Value 8.3 N/mm2, Test Method - ASTM C 580
• Tensile Strength: 5.5 N/mm2, Test method - ASTM C 307
• Impact Resistance: No sign of Crack or Disbonding observed, Test Method - ASTM ISO 6272
• Crack Bridging Capacity: Value -1.35 mm, Test Method - ASTM C 836:95
• Rapid Chloride Permeability: Value = 99% Reduction, Test Method - ASTM C 1202.97
• Water Permeability - BS EN 12390 (PART 8 : 2000)
• Chemical Resistance: No change observed, Test Method - ASTM D 543
• Hot Water Resistance: No change observed, Test Method - ASTM D 570
• Abrasion resistance: 107 gms weight Lost after 1000 Cycles ( 1 kg Load CS-17 Wheel) Test
Method - ASTM D 4060 : 01

Designed Use
• Seamless floorings for showrooms, business centres, malls
• Easy clean coating to kitchen and poultries.
• Pharmaceutical units, food processing plants and chemical plants.
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