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	SYSTEM : PU BASED FLOOR COATING FOR TRAFFIC ENVIROMENT, RAMPS, CAR PARKS, WALKWAYS AND STEPS

	Floor- MD Indoor and Outdoor



System Description

Primary Coat: 1 coat of Apcoflor FP 100 Clear @ 50 μ
Two component, high solid, epoxy resin based universal floor primer.

Volume Solids: 62% ± 2%

Secondary Coat: 2 coats of Apcoflor TC-510 @ 250 μ 
Two components, high build, solvent free, epoxy floor coating.

Volume Solids: 100% (Based on ASTM D2697)
VOC: 3.9 gms/ltr, Test Method USEPA 24

Top Coat: 1 coat of Apcoflor TC 600 @ 50 μ 
A two pack acrylic polyol and aliphatic isocyanate based Polyurethane floor topcoat.

Volume Solids: 45% ± 2%

Certificate
• Shore ‘D’ Hardness: D/65/1, Test method - ASTM D 2240
• Compressive Strength - 70.1 N/mm2, Test method - ASTM C 579
• Flexural Strength: 40.1 N/mm2, Test method - ASTM C 580
• Tensile Strength: 20.1 N/mm2, Test method - ASTM C 307
• Impact Resistance: No sign of crack or disbonding observed, Test method - ASTM ISO 6272
• Crack Bridging Capacity: Value -1.20 mm, Test method - ASTM C 836:95
• Rapid Chloride Permeability: 93% reduction, Test method - ASTM C 1202.97
• Water Permeability: Nil, Test method - BS EN 12390 (PART 8 : 2000)
• Chemical Resistance: No change observed, Test method - ASTM D 543
• Hot Water Resistance: No change observed, Test method- ASTM D 570
• Abrasion Resistance: 185 gms weight Lost after 1000 Cycles ( 1 kg Load CS-17 Wheel)
Test Method - ASTM D 4060 : 01

Designed Use
• Easy clean floor coating for food processing plants, soft drink plants
• Seamless automotive plants, warehouses and chemical plants.
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