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	SYSTEM : PU BASED FLOOR COATING FOR RAMPS, WALKWAYS AND STEPS

	Floor- MD Indoor/Outdoor, Car Park Ramp and Exposed Area



System Description

Primary Coat: 1 coat of Luxaflor 1100 @ 50 μ
A high performance two pack epoxy primer specially designed to penetrate into, and seal the surface of concrete. Provides sound base for improved adhesion of subsequent Berger epoxy or polyurethane based floor coating.

Volume Solids: 45% ± 2%

Secondary Coat: 2 coats of Luxaflor 4000 @ 150 μ
A two pack modified amine based epoxy coating with excellent resistance to abrasion and to fresh and salt water, non oxidizing acids, oils and many other chemicals.

Volume Solids: 78% ± 2%

Top Coat: 1 coat of Luxaflor 4100 @ 50 μ
A two pack acrylic polyol and aliphatic isocyanate based polyurethane floor topcoat.

Volume Solids: 45% ± 2%

Designed Use
[image: ]• As an abrasion resistant floor coating for moderate traffic environments.
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