SYSTEM : DESIGNER FINISH FOR INTERIOR – ROYALE PLAY SAFARI

Concrete and Masonry surface - Interior

System Description:

Primary Coat: 1 coat of Berger Alkali Resistance Primer

A premium quality alkali resisting primer based on an acrylic co-polymer designed to penetrate into, and seal the surface.

Volume Solids: 25 ± 2%

VOC: <0.01(g/L) (Test Method -USEPA 24)

Estidama QCC approved

Conform to MPI 3

Alkali Resistance Test - MPI 50

Secondary Coat: 2 coats of Berger Value Stucco

An acrylic co-polymer based filler containing alkali resisting pigments, for the filling of surface irregularities and indentations, hairline surface cracks etc.

Volume Solids: 52% ± 2%

VOC: Near 0 (Test Method - ISO 11890 - 1)

Estidama QCC approved

Conform to MPI 4

Third Coat: 2 coats of Berger Royale Premium Matt Emulsion

A premium emulsion with excellent washability and scrub resistance, resistance to fungus and algae, offering a smooth, matt finish.

Volume Solids: 35 % ± 2 %

VOC: 0.01 gms/ltr as per USEPA 24 (Complies to LEED Standard)

Features - Lead Free, Low Odour, Alkali Resistant & Heavy Metals free

Top Coat: 1 or 2 coats of Berger Royale Play Safari depending on the design

Water-based special effects paint that creates a variety of special effects on the interior walls.

Volume Solids: 45 % ± 2 %

VOC: <10 gms/ltr complies to LEED Standard (Near 0 VOC)

Features - Low Odour, Lead Free, Alkali Resistant

Areas of Application

Area of Use: Interior

Substrate: Concrete, Plaster, Masonry, Gypsum, Timber