SYSTEM: DESIGNER FINISH FOR INTERIORS - ROYALE PLAY METALLIC GLAZE

Concrete and Masonry Surface - Interior

System Description

Primary Coat: 1 coat of Berger Royale Alkali Resistance primer

A premium quality alkali resisting primer based on an acrylic co-polymer designed to penetrate into, and seal the surface.

Volume Solids: 25 ± 2%

VOC: <0.01(g/L) (Test Method -USEPA 24)

Estidama QCC approved

Conform to MPI 3

Alkali Resistance Test - MPI 50

Secondary Coat: 2 coats of Berger Value Stucco

An acrylic co-polymer based filler containing alkali resisting pigments, for the filling of surface irregularities and indentations, hairline surface cracks etc.

Volume Solids: 52% ± 2%

VOC: Near 0 (Test Method - ISO 11890 - 1)

Estidama QCC approved

Conform to MPI 4

Third Coat: 2 coats of Berger Royale Premium Silk Emulsion

A premium emulsion with outstanding scrub resistance and washablility, resistance to fungus and algae, easy cleaning properties, dust resistance and an appealing smooth finish with a silky sheen.

Volume Solids: 44 % ± 2 %

VOC: <24 gms/ltr complies to LEED Standard

Features - Lead Free, Low Odour, Alkali Resistant & Heavy Metals free

Top Coat: 1 to 2 coats of Berger Royale Play Metallic Glaze depending on the design

Water-based special effects paint that creates a variety of special metallic effects on interior walls.

Volume Solids: 26 % ± 2 %

VOC: <10 gms/ltr complies to LEED Standard (Near 0 VOC)

Features - Low Odour, Lead Free, Alkali Resistant

Areas of Application

Area of Use: Interior

Substrate: Concrete, Plaster, Masonry, Gypsum, Timber