SYSTEM : ANTI MICROBIAL EGGSHELL INTERIOR WASHABLE SYSTEM - SILK FINISH

Concrete and Masonry Surface - Interior

System Description

Primary Coat: 1 Coat of Berger Alkali Resistance Primer

A premium quality alkali resisting primer based on an acrylic co-polymer designed to penetrate into, and seal the surface.

Volume Solids: 25 ± 2%

VOC: <0.01(g/L) (Test Method -USEPA 24)

Estidama QCC approved

Conform to MPI 3

Alkali Resistance Test - MPI 50

Secondary Coat: 2 Coats of Berger Value Stucco

An acrylic co-polymer based filler containing alkali resisting pigments, for the filling of surface irregularities and indentations, hairline surface cracks etc. It helps to produce a smooth and level surface prior to painting.

Volume Solids: 52% ± 2%

VOC: Near 0 (Test Method - ISO 11890 - 1)

Estidama QCC approved

Conform to MPI 4

Top Coat: 2 Coats of Berger Select Eggshell Silk Emulsion

A silk finish based acrylic co-polymer containing titanium dioxide and other high grade light-fast alkali resisting pigments. It has outstanding scrub resistance and washability, and resistance to fungus and algae.

Volume Solids: 34 % ± 2 %

VOC: <10 gms/ltr complies to LEED Standard (Near 0 VOC)

• Estidama QCC Approved

• >5000 Scrub Cycle ASTM D 2486

• Heavy metals free

• Estidama QCC Approved

• Anti Microbial: Rating - 10 (Test Method ASTM - D3273 - 94)

Areas of Application

Area of Use: Interior

Substrate: Concrete, Plaster, Masonry, Gypsum, Timber