SYSTEM : PU COATING FOR GALVANIZED IRON

Surface – GI

System Description

Primary Coat: 1 coat of Luxaprime 1500 @ 5μ

A two pack polyvinyl butyral primer containing phosphoric acid and corrosion inhibitive pigments also known as Wash Primer.

• BS 5493 reference. Meets performance of AP2A

Volume Solids: 8.5% ± 0.5%

LEAD CONTENT- ASTM D3618, Value - less than 0.05%

Secondary Coat: 1 coat of Epimastic 5100@100μ

A high solids high build low VOC self-priming aluminium flaked anticorrosive epoxy coating which can be applied to galvanized steel and old or new steel following the removal of loose rust and scale.

Volume Solids: 82% ± 2%

VOC: <EPA 24 A, 239 gms/ltr

Top Coat: 1 coat of Luxathane 5160@75μ

A two component acrylic polyurethane giving a high performance finish in new construction and maintenance industries.

• Conforms to BS 5493 - KF2A

Volume Solids: 63% ± 2%

Certificates

Abrasion resistance - Value -99.55 mg CS17 wheel with 1 Kg load, Test Method – ASTM D4060

Pull-off test - Value-7.96 Mpa, Test Method - ASTM D 4060

Salt spray - Passes 1000 hrs with suitable primers, Test Method - ASTM B 117 - 07A

Designed Use

• As a topcoat for the exterior of chemical storage tanks, pipelines.

• Suitable for application on structural steel, tanks and piping for onshore and offshore facilities

• Suitable as topcoat for upto C5 Environment as per ISO12944 Part 2.