SYSTEM : PREMIUM FINISH FOR WOOD - INTERIOR /EXTERIOR (CLEAR )

Wood - Exterior (Clear)

Primary Coat: 2-3 coats of Touchwood Acrylic PU Sanding Sealer

Based on acrylic resin isocyanate. Has excellent grain filling properties and weather resisting properties when  topcoated with touchwood acrylic 2k PU.

Volume Solids: 32% ± 2%

Top Coats: 1-2 coats of Touchwood Acrylic PU Topcoat (Clear)

Ultra premium quality two-pack composition based on acrylic resin isocyanate. The product has been designed to withstand very aggressive physical and chemical environment like abrasion, heat, light, alcohol, tea hot/beverages, nail enamel and almost all aliphatic/aromatic solvents.

% Solids (NVM): 43% ± 2%

Certificates

Touchwood Acrylic PU Sanding Sealer with Touchwood Acrylic PU Top Coat is a FIRA Approved System.

Recommended Areas of Application

Area of Use: Interior and Exterior

Substrate: Wood and related substrates