SYSTEM : LOW (VOC) PREMIUM FINISHES FOR WOOD - INTERIOR

Wood –Interior (Clear) Low - VOC

Primary Coat:  2-3 coats of Touchwood (Low VOC) PU Sanding Sealer Interior

Based on acrylic resin isocyanate which has excellent grain filling properties.

Volume Solids: 46% ± 2%

VOC: <275 gms/ltr complies to LEED Standard

Top Coats: 1-2 coats of Touchwood PU Topcoat (Low VOC) - Clear

A two pack polyurethane coating based on suitably modified polyester containing special additives to provide a smooth, tough, durable and hardwearing finish with good flow and film build-up. This Product has Low VOC

Highlights:

• Excellent leveling and very fast drying

• Gloss/Silk Matt/Matt finish with good hardness

• Good resistance to household chemicals and beverages

Volume Solids: 47% ± 2%

VOC: <275 gms/ltr complies to LEED Standard

Certificates

ESTIDAMA QCC APPROVED

Recommended Areas of Application

Area of Use: Interior only

Substrate: Wood and related substrates