PREMIUM FINISH FOR WOOD - INTERIOR (PIGMENTED)

Wood - Interior (Pigmented)

Primary Coat: 1-2 coats of Touchwood PU Primer

Two pack polyurethane based on suitably modified polyester containing zinc stearate, titanium dioxide and in combination with suitable catalyst provides a tough, durable and hard wearing film.

Volume Solids: 56% ± 2%

Top Coats: 1-2 coats of Touchwood PU Topcoat (Pigmented)

A two pack polyurethane coating based on suitably modified polyester containing special additives to provide a smooth, tough, durable and hardwearing finish with good flow and film build-up.

Highlights

• Excellent leveling and very fast drying

• Gloss/ Silk Matt/ Matt finish with good hardness

• Good resistance to household chemicals and beverages

Volume Solids: 62% ± 2%

Recommended Areas of Application

Area of Use: Interior only

Substrate: Wood and related substrates