SYSTEM : ANTI MICROBIAL EGGSHELL INTERIOR WASHABLE SYSTEM - MATT FINISH

Concrete and Masonry surface - Interior

System Description

Primary Coat: 1 Coat of Berger Alkali Resistance Primer

A premium quality alkali resisting primer based on an acrylic co-polymer designed to penetrate into, and seal the surface.

Volume Solids: 25 ± 2%

VOC: <0.01(g/L) (Test Method -USEPA 24)

Estidama QCC approved

Conform to MPI 3

Alkali Resistance Test - MPI 50

Secondary Coat: 2 Coats of Berger Value Stucco

An acrylic co-polymer based filler containing alkali resisting pigments, for the filling of surface irregularities and indentations, hairline surface cracks etc.

Volume Solids: 52% ± 2%

VOC: Near 0 (Test Method - ISO 11890 - 1)

Estidama QCC approved

Conform to MPI 4

Top Coat: 2 Coats of Berger Select Eggshell Matt Emulsion

A high quality acrylic co-polymer latex pigmented with titanium dioxide and other light fast and alkali resisting pigments.

Volume Solids: 35 % ± 2 %

VOC: <10 gms/ltr complies to LEED Standard (Near 0 VOC)

• Estidama QCC Approved

• >3000 Scrub Cycle ASTM D 2486

• Heavy metals free

• Estidama QCC Approved

• Anti Microbial: Rating - 10 (Test Method ASTM - D3273 - 94)

Areas of Application

Area of Use: Interior

Substrate: Concrete, Plaster, Masonry, Gypsum, Timber