SYSTEM : PREMIUM FINISH FOR WOOD - INTERIOR/ EXTERIOR (PIGMENTED)

Wood - Exterior (Pigmented)

Primary Coat: 1-2 coats of Touchwood acrylic PU primer

Two pack polyurethane based suitably modified polyester containing zinc stearate, titanium dioxide and in combination with suitable catalyst provides a tough, durable and hard wearing film.

Volume Solids: 56% ± 2%

Top Coats: 1-2 coats of Touchwood acrylic PU Topcoats Pigmented

The product has been designed to withstand very aggressive physical and chemical environment like abrasion, heat, light, alcohol, tea hot/beverages, nail enamel and almost all aliphatic/aromatic solvents.

% Solids (NVM): 57% ± 2%

Certificate

Touchwood Acrylic PU Sanding Sealer with Touchwood Acrylic PU Topcoat is a FIRA Approved system.

Recommended Areas of Application

Area of Use: Interior only

Substrate: Wood and related substrates